ORDINANCE 57

SECTION II

SUBSECTION I

SPECIFICATIONS FOR THE SIDEWALK ORDINANCE

- Sidewalks to keep free of snow and ice:  Only sidewalks abutting the business streets will be enforced as to snow and ice.  If complaints are heard about any residential area, the matter will be looked into then.

- Sidewalk construction: All city sidewalks must be of concrete, six bag mix or better.  All new construction of city sidewalks will be a minimum of 4’ in width, 4" thick with a minimum of 4” compacted granular material subgrade, and a contraction joint cut every 4' except where there is a driveway, and a ½” expansion joint at walk or structure.  Where there is a driveway the sidewalk must be a minimum of 6” thick.  Any driveways put in must not go above the sidewalk grade.  All grades of sidewalks will be uniform to the roadway or to the uniform grade of the said block it is being laid on.  All sidewalks approaching a roadway will have a downward grade in a way so as not to prohibit the flow of water and at a pitch of 1-12 or less.  All roadway connections that have a curb will cut and replace with a handicapped ramp of not more than 1-12 pitch.  All new construction will be inspected by the City Maintenance Department before the concrete is laid.

- Repairs:  All repairs will be done with suitable concrete materials.  Any hole of 5" square or bigger at a depth of 1/4" or greater must be repaired.  Any grade of less than 1-12 pitch or 4" above grade surface must be replaced to follow grade of sidewalk.  Any vertical displacement of 1/2" or greater must be repaired to less than 1-12 pitch.

- Trees, Shrubs and Fences:  Any trees, shrubs or fences planted or erected near any public road or sidewalk will be done so as not to obstruct view of any traffic.  All roadway and sidewalks must maintain a minimum height of 12' above grade and maintained to give sidewalk width of 2' from edge of sidewalk or 20' from roadway.  All dead trees or shrubs, or parts of, must be removed.

- Inspection:  There will be an inspection once a year by the City Maintenance Department.

Revision approved April 3, 2017.			Mayor, Raye Ludovissie

Published April 13, 2017 in the Verndale Sun	Clerk, Barbara Holmes